VALMOND & GIBSON  |  Specification Clause

165CW — Unitised Curtain Wall System — Section 0413 Curtain Walls

________________________________________________________________________________

## 1  GENERAL

### 1.1  Scope

Supply of unitised aluminium curtain wall system including framing, glazing adaptors, brackets, and associated components.

### 1.2  Referenced Documents

-  AS/NZS 1170.0:2002 — Structural design actions, General principles

-  AS/NZS 1170.2:2021 — Structural design actions, Wind actions

-  AS/NZS 1866:1997 — Aluminium and aluminium alloys

-  AS/NZS 4284:2008 — Testing of building facades

-  AS 3715:2002 — Metal finishing — Thermoset powder coatings

-  AS 1231:2000 — Aluminium and aluminium alloys — Anodic oxidation coatings

-  AS 1288 — Glass in buildings

-  NCC — National Construction Code, Volume 1

### 1.3  Submissions

Submit to the Superintendent for review:

-  System data including frame sections, thermal performance, and structural capacity

-  Structural engineering certification for project-specific wind loads

-  Colour samples for approval

-  Shop drawings showing unit layout, stack joints, mullion details, bracket details

-  Glazing schedule

-  Movement accommodation details (stack head and mullion)

-  Warranty documentation

## 2  PRODUCTS

### 2.1  Manufacturer

Valmond & Gibson Pty Ltd

Product: 165CW Unitised Curtain Wall System

Designed, engineered, and extruded in Australia

Tel: 1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com

### 2.2  System Specifications

| Property | Specification |
| --- | --- |
| Frame depth | 165mm internal |
| Mullion width | 86mm (including 10mm nominal gap) |
| Primary framing alloy | 6060-T6 |
| Secondary framing alloy | 6060-T5 |
| Structural members | 6005A-T6 |
| IGU glazing capacity | 24mm to 40mm |
| Stack head movement | ±25mm |
| Mullion movement | ±10mm |
| Glazing method | 4-side structural silicone |

### 2.3  Key Features

-  Thermally broken glazing adaptors (polyamide strip with aluminium nose cap)

-  Integrated horizontal and vertical sunshade brackets with concealed nutplate

-  3-part structural bracket with 3D installation adjustment

-  Hook-on bracket system for unitised installation

-  Curved panel capability (via partner facility)

-  Integrated architectural skirting and blind pelmet options

### 2.4  Conforming Standards

-  AS/NZS 1170.0 — Structural design actions

-  AS/NZS 1866 — Aluminium extrusion tolerances

-  AS/NZS 4284 — Facade testing

-  AS 3715 — Powder coat finishes

-  AS 1231 — Anodic oxidation coatings

### 2.5  Finish

[Select: Powder coat / Anodised]

[Specify colour name or reference]

### 2.6  Software

V&G 165CW is supported by a dedicated LogiKal (Orgadata) database for estimating, cutting optimisation, AutoCAD export, and CNC machine control.

## 3  EXECUTION

### 3.1  Installation

Install in accordance with the 165CW Technical Manual (188 pages) and approved shop drawings.

-  Unitised panels to be installed using hook-on bracket system

-  Structural brackets to provide 3D adjustment for building tolerances

-  Stack head and mullion joints to accommodate specified movement

-  All connections using #12 assembly screws

-  Glazing in accordance with AS 1288 and IGU manufacturer's requirements

## 4  WARRANTY

Warranty terms per V&G standard warranty conditions, covering manufacturing defects in framing, hardware, and finish.

________________________________________________________________________________

This specification clause is provided by Valmond & Gibson Pty Ltd as guidance for project specifications. It should be reviewed and adapted by the specifier to suit the specific project requirements.

Valmond & Gibson Pty Ltd  |  ABN 99 628 654 605

23-25 Princes Road East, Auburn NSW 2144

1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com