VALMOND & GIBSON  |  Specification Clause

conneQt — Aluminium Batten & Adaptor System — Section 0612 Metal Cladding

________________________________________________________________________________

## 1  GENERAL

### 1.1  Scope

Supply of aluminium battens, adaptors, and architectural screening elements.

### 1.2  Referenced Documents

-  AS 1530.1:1994 — Combustibility test for materials

-  AS/NZS 1170 — Structural design actions

-  AS/NZS 1866:1997 — Aluminium and aluminium alloys — Extrusion tolerances

-  NCC — National Construction Code, Volume 1

### 1.3  Submissions

Submit to the Superintendent for review:

-  Product data sheets

-  Combustibility test certificate (AS 1530.1)

-  Colour samples for approval

-  Shop drawings showing batten layout, fixing centres, and connection details

## 2  PRODUCTS

### 2.1  Manufacturer

Valmond & Gibson Pty Ltd

Product: conneQt Aluminium Batten & Adaptor System

Tel: 1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com

### 2.2  Materials

| Property | Specification |
| --- | --- |
| Alloy | 6060/6063, T5 temper |
| Profile types | Vertical battens, horizontal battens, architectural fins, screening elements |
| Density | 2,680 kg/m³ |

### 2.3  Performance Requirements

Non-combustible when tested to AS 1530.1:1994 (solid extruded aluminium — inherently non-combustible).

Structural design to AS/NZS 1170 for project-specific wind loads.

### 2.4  Compatibility

conneQt is designed for integration with interloQ rainscreen cladding and element13 solid panels. Same alloy family (6060/6063) and available in matching finishes for colour consistency across combined facade systems.

### 2.5  Finish

[Select: Powder coat / Anodised]

[Specify colour — match to interloQ or element13 finish if combined facade]

## 3  EXECUTION

### 3.1  Installation

Install in accordance with approved shop drawings and V&G fixing guidance.

-  Fix battens to supporting framework at centres per structural requirements

-  Maintain consistent spacing and alignment across facade

-  Do not weld — use mechanical fixings only

## 4  WARRANTY

Warranty per V&G standard warranty conditions, covering manufacturing defects in material and finish.

________________________________________________________________________________

This specification clause is provided by Valmond & Gibson Pty Ltd as guidance for project specifications. It should be reviewed and adapted by the specifier to suit the specific project requirements.

Valmond & Gibson Pty Ltd  |  ABN 99 628 654 605

23-25 Princes Road East, Auburn NSW 2144

1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com