VALMOND & GIBSON  |  Specification Clause

element13 — Solid Aluminium Cladding Panels — Section 0612 Metal Cladding

________________________________________________________________________________

## 1  GENERAL

### 1.1  Scope

Supply of solid aluminium cladding panels and associated fixings.

### 1.2  Referenced Documents

-  AS 1530.1:1994 — Combustibility test for materials

-  AS 1530.3:1999 — Simultaneous determination of ignitability, flame propagation, heat release and smoke release

-  AS/NZS 4284:2008 — Testing of building facades

-  ASTM E695-03 — Impact resistance of wall assemblies

-  AAMA 2605:2020 — Voluntary specification for high performance coatings on metal substrates

-  ANSI FM 4473 — Hail impact resistance

-  NCC — National Construction Code, Volume 1

### 1.3  Submissions

Submit to the Superintendent for review:

-  Product data sheets including material specifications and tolerances

-  Test certificates: AS 1530.1 combustibility (CSIRO report FNC12545)

-  Test certificates: AS 1530.3 fire performance (CSIRO report FNE12552)

-  Test certificates: AS/NZS 4284 weather performance (report 2022-031-S2)

-  Test certificates: Wind load structural testing (JFS Engineers report 23-00156)

-  Test certificates: Impact resistance ASTM E695 (report 2021-083_2)

-  Coating test certificate: AAMA 2605 (Intertek report 210203002SHF-001)

-  Colour samples for approval (minimum 200mm x 200mm)

-  Shop drawings showing panel layout, fixing details, joint details

-  Warranty documentation

## 2  PRODUCTS

### 2.1  Manufacturer

Valmond & Gibson Pty Ltd

Product: element13 Solid Aluminium Cladding Panels

Tel: 1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com

### 2.2  Materials

| Property | Specification |
| --- | --- |
| Material | 3mm solid aluminium panel |
| Width | 1250mm or 1500mm |
| Length | 3200mm or 4000mm |
| Weight | 8.13 kg/m² |
| Coating | PPG PVDF paint finish (AAMA 2605 compliant) |
| Manufacturing QMS | ISO 9001:2015 |

### 2.3  Tolerances

| Dimension | Tolerance |
| --- | --- |
| Width (≤1500mm) | ±2.0mm |
| Length (3000-3600mm) | ±4.0mm |
| Length (3600-4500mm) | ±4.0mm |
| Thickness | ±0.18mm |

### 2.4  Performance Requirements

| Requirement | Standard | Evidence |
| --- | --- | --- |
| Non-combustible | AS 1530.1:1994 | CSIRO report FNC12545 |
| Fire properties | AS 1530.3:1999 | CSIRO report FNE12552 — Ig 0, Flame 0, Heat 0, Smoke 1 |
| Weather performance | AS/NZS 4284:2008 | Report 2022-031-S2, ±1500Pa SLS |
| Structural (wind) | AS 4040.3 (cyclonic) | JFS report 23-00156 — SLS 1875Pa, ULS 5559Pa |
| Impact resistance | ASTM E695-03 | Report 2021-083_2 — Pass |
| Surface indentation | NCC C1.8 Clause 5(d) | Report 2021-083 — Immeasurable |
| Coating performance | AAMA 2605:2020 | Intertek report 210203002SHF-001 |
| Hail impact | ANSI FM 4473 | Report 2020-090 — Pass |

### 2.5  Colour

[Specify colour from element13 colour range — solid, metallic, woodgrain, or custom]

Refer to element13 colour chart for stock and non-stock options. Non-stock colours subject to minimum order quantities.

## 3  EXECUTION

### 3.1  Installation

Install in accordance with the element13 Technical Manual (44 pages) and approved shop drawings.

-  Panels to be fixed using concealed fixing system per approved details

-  Joint widths and sealant to architect's detail

-  Panels to be handled with clean gloves to prevent marking

-  Protect cut edges and drilled holes from corrosion where required

### 3.2  Cleaning

Clean every 3 months with mild detergent and warm water. More frequent cleaning in coastal or industrial environments. Do not use solvents on PVDF-coated surfaces.

## 4  WARRANTY

Warranty: Up to 20 years covering substrate and coating, when installed by a qualified installer.

________________________________________________________________________________

This specification clause is provided by Valmond & Gibson Pty Ltd as guidance for project specifications. It should be reviewed and adapted by the specifier to suit the specific project requirements.

Valmond & Gibson Pty Ltd  |  ABN 99 628 654 605

23-25 Princes Road East, Auburn NSW 2144

1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com