VALMOND & GIBSON  |  Specification Clause

interloQ — Interlocking Aluminium Rainscreen Cladding — Section 0612 Metal Cladding

________________________________________________________________________________

## 1  GENERAL

### 1.1  Scope

Supply of interlocking aluminium rainscreen cladding panels, battens, and associated fixings.

### 1.2  Referenced Documents

-  AS 1530.1:1994 — Combustibility test for materials

-  AS/NZS 4284:2008 — Testing of building facades

-  AS/NZS 1170 — Structural design actions (General, Wind, Earthquake)

-  AS/NZS 1866:1997 — Aluminium and aluminium alloys — Extrusion tolerances

-  AS 3715:2002 — Metal finishing — Thermoset powder coatings

-  AS 1231:2000 — Aluminium and aluminium alloys — Anodic oxidation coatings

-  NCC — National Construction Code, Volume 1

### 1.3  Submissions

Submit to the Superintendent for review:

-  Product data sheets including material specifications

-  Test certificates: AS 1530.1 combustibility (CSIRO report FNC12595)

-  Test certificates: AS/NZS 4284 weather performance (report 2022-031-S1)

-  Colour samples for approval (minimum 100mm x 100mm)

-  Shop drawings showing panel layout, fixing details, and flashing details

-  Installation methodology statement

-  Warranty documentation

## 2  PRODUCTS

### 2.1  Manufacturer

Valmond & Gibson Pty Ltd

Product: interloQ Interlocking Aluminium Rainscreen Cladding

Tel: 1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com

### 2.2  Materials

| Property | Specification |
| --- | --- |
| Alloy | 6060/6063, T5 temper |
| Thickness | 1.8 - 3.5mm (select per structural requirements) |
| Density | 2,680 kg/m³ |
| Tensile strength (ultimate) | 180 MPa |
| Tensile strength (yield) | 140 MPa |
| Modulus of elasticity | 68 GPa |
| Thermal expansion | 23 µm/m/°K |
| Melting range | 616 - 654°C |

### 2.3  Performance Requirements

The cladding system shall meet the following performance requirements:

| Requirement | Standard | Evidence |
| --- | --- | --- |
| Non-combustible | AS 1530.1:1994 | CSIRO report FNC12595 (NATA lab #165) |
| Weather performance | AS/NZS 4284:2008 | Report 2022-031-S1, ±1500Pa SLS (NATA lab #2371) |
| Structural design | AS/NZS 1170 | Engineering certification to project wind loads |
| Extrusion tolerances | AS/NZS 1866:1997 | Manufacturer quality system |

### 2.4  Finish

Select finish type:

[Select: Powder coat / Anodised / Woodgrain effect / Custom colour]

Powder coat: Interpon D2525 standard range or Structura textured range.

Anodised: Natural, Bronze, or Black.

Colour:

[Specify colour name or reference]

### 2.5  Panel Configuration

Orientation:

[Select: Vertical / Horizontal]

Panel profile:

[Specify profile width — refer to interloQ Technical Manual for available profiles]

## 3  EXECUTION

### 3.1  Installation

Install in accordance with the interloQ Technical Manual (67 pages) and approved shop drawings.

-  Fix panels with rivets or screws to supporting framework

-  Maintain ventilated drainage cavity behind panels — minimum depth per approved details

-  Panels to be installed with interlocking connection engaged along full length

-  Do not weld panels — heat will damage coating and compromise T5 temper

-  Pre-punched fixing slots to be used for standard fixing locations

-  Weather-resistant barrier (sarking) to be installed to cavity face of supporting wall prior to cladding installation

### 3.2  Protection

Protect installed panels from damage by subsequent trades. Cover exposed panels with protective film where risk of impact, scratching, or mortar/paint splatter exists.

### 3.3  Cleaning

On completion, clean all panels with mild detergent and warm water. Do not use solvents or turpentine on powder-coated surfaces. Isopropyl alcohol or methylated spirits acceptable for spot cleaning.

## 4  WARRANTY

Warranty: Up to 20 years covering substrate and coating, when installed by a qualified installer.

Warranty covers manufacturing defects in material and finish. Refer to V&G warranty terms for full conditions, exclusions, and maintenance requirements.

________________________________________________________________________________

This specification clause is provided by Valmond & Gibson Pty Ltd as guidance for project specifications. It should be reviewed and adapted by the specifier to suit the specific project requirements.

Valmond & Gibson Pty Ltd  |  ABN 99 628 654 605

23-25 Princes Road East, Auburn NSW 2144

1300 097 999  |  sales@valmondgibson.com  |  valmondgibson.com